Blue Celadon Glaze Custer Feldspar 44.0 Silica 20.0 Kaolin (Grolleg) 12.0 Wollastonite 20.0 Dolomite 4.0 Red Iron Oxide 2.0

Reitz Green Nepheline Syenite 70.0 Petalite 15.0 Whiting 5.0 Ball Clay 8.0 Gerstley Borate 2.0 Rutile 2.0 Cobalt Carbonate 1.0

Blue Celadon Glaze

Blue Celadon Glaze

Reitz Green Glaze

Reitz Green Glaze